**Creative Clothex, Noida - VISIT REPORT**

**Visit Date** – **10th – 12th April, 2015**

**Visiting Executives from JCT Phagwara** – Mr. Husan Lal (DGM- Taffeta Plant) & Mr. Kishor Chand (Manager-R&D, QA).

**Contact Person at Creative Clothex** –Mr. Mohit Singhal, Ms. Gurvinder, Mr. Abhikaran Sharma, Mr. Mohit Sharma.

**Agenda** – To attend Fabric Quality Complaint in JCT supplied fabrics – **DYM-22085 for Needle Yarn Pulling near Selvedge & Slub Issue , DPM-22428 for Slub issue & 22169 for Slub & Hazy look.**

**Brief Minutes of Meeting are as under:**

We have visited M/s Creative Clothex, Noida and inspected total supplied fabric in presence of Mr. Abhikaran Sharma, Mr. Mohit Sharma & Mr.Vaibhav from adidas (LO). Summary of the same is as under.

***Sort No. DYM22085* (PO – 2222/2015)**

1. **Needle Yarn Pulling Near Selvedge: -** In Sort no. DYM22085, we have inspected 2 rolls (81677-164m, 81678-85m) of shade Vista Blue and one roll 83162-198m of shade Collegiate Navy for needle yarn pulling, where yarns pulling on both sides near selvedge at random places have been observed. Useable width after deducting 4inches (2inches from both sides) from width had 52inches against required 56”. Customer is asked for replenishment to compensate excess consumption by 10% on avoid & cut basis. Hence, agreed to give 10% FOC fabric to compensate excess consumption. Shade wise FOC breakup as under.

**Invoice No. Shade Fabric Dispatch FOC to be given**

NINV/145902/2015 Black 1890m 199m

NINV/146261/2015 ”

NINV/146476/2015 “

NINV/147537/2015 “

NINV/145902/2015 Collegiate Navy 1620m 152m

NINV/145780/2015 Vista Blue 518 52m

1. **Slub & Patchiness (uneven weft): -** In Sort no. DYM22085\_shade Collegiate navy, out of total 1620m fabric supplied, customer was complaint one roll no. 83162-198m fabric having defect of weft patta (unevenness). We have inspected same roll, where only 70m weft patta (unevenness) has been observed in total fabric roll 198m. TO compensate the excess fabric consumption, agreed to give 30m fabric on FOC basis to the customer.
2. **Warp Streaks -** In Sort no. DYM22085\_shade Vista Blue, out of total 518m fabric supplied, customer was complaint for Warp direction streaks in all fabric. We have inspected 2 rolls (81677-164m, 81678-85m) of shade Vista Blue for warp streaks. In roll no. 81677- 164m, major warp streaks at 2-3 places in warp direction have been observed in 24m fabric and roll no. 81678- 85m, major streaks in full roll have been observed. Out of 518m fabric, 109m fabric will be replaced against the return of 109m fabric to complete the invoice order quantity and rest fabric has been approved by adidas LO for minor streaks.

***Sort No. DPM22428* (PO – PLN000053/2015, Invoice No. –To confirm\_ Shade Collegiate NavyQuantity-313m)**

**Slubs Problem: -** We have inspected 1 roll (19530-86m) for shade Collegiate Navy, where full roll having slubs in 15-20” from the one side of selvedge which is not useable. Hence, agreed to replace total 313m fabric against the return of 313m fabric.

***Sort No. DYM 22169* (PO – PLN000067/2015, Invoice No. NINV -148221/2015\_Shade CH Solid Grey\_ Quantity-867m)**

**Slub & Patchiness (uneven weft): -** Out of total fabric supplied fabric 867m of shade collegiate navy in above said invoice, customer was rejected one roll no. 21625-167m fabric for slub and patchiness. We have inspected same roll and observed slub/unevenness in the fabric but it was seams OK as per approved sample recd. from adidas LO. As Mr. Vaibhav of adidas office was there and shown the same to him and he taken sample with him. He asked to give decision on 13/4/2015 (Monday) after discussion with Mr. Anurag Bhaskar. On Monday, April 13, 2015, they have rejected 167m fabric and advice to replace 167m fabric. We have discussed with Mr. Anurag Bhaskar on phone again and will give decision after making garment.

Overall Brief Summary Break up for Replenishment (FOC & Replacement)

**Sort No. Shade FOC Replacement Total (FOC+Replacement)**

**Quantity (m) Quantity (m) Quantity (m)**

22085 Black 199 Nil 199

“ Colleg. Navy 182 Nil 182

“ Vista Blue 52 109 161

---------------------------------------------------------------------------------------------------

Total 433 109 542

22428 Colleg. Navy Nil 313 313

22169 CH Solid Grey Nil Decision pending with Adidas LO

Best Regards,

(Husan Lal) (Kishor Chand)

(DGM- Taffeta Plant) (Manager-R&D, QA)