**Customer-First Garment Manufacturing (Decathlon)**

**DBW22298 (P190T),**

**Shade- Crimson Red, Dark Navy**

**Invoice no – 148716, 142302**

**PO- RMG-3506, 454,**

**Total Quantity- 13877m**

**(Rejection Period- June, July & August’15 i.e 3 Months)**

**Fabric Rejected -487.5 (Replacement 447m + FOC 40.5m)**

**Issue – Weaving & Coating Over points**

1. **During visit of Mr. Chandwani and under signed on dated 12/9/2015, in Sort no. 22298DBW (P190T), FGM has rejected 756m fabric due to over points. After rejected fabric seen and discussion, FGM agreed on to use the fabric as under.**

**For rejection fabric 117mtr, ( 20 to 25 points ) FOC @ 10% is 11.7mtrs will be given.**

**For rejection fabric 192mtr, ( 25 to 30 points ) FOC @ 15% is 28.8mtrs will be given.**

**And rejection fabric 447mtr, (above 30 points) FGM can’t use fabric and will be given replacement against the return of 447m fabric in JCT**

**Overall Summary:- 40.5m (11.7+28.8m) fabric will be given as FOC against the use of excessive point fabric and 447m fabric will be replacement against the return of fabric in the JCT only. Total Fabric required (11.7+28.8+447=487.5m). 487.5m fabric will be given in one shade i.e. Dark Navy.**

**Note:- Replacement of fabric will be give subjected to actual fabric recd. in the JCT and color required according to customer need.**